Green sustainable method for water and soil purification: Photo-degradation of soil- and water- organic contaminants using semiconductor nano-particles

Zyoud A. H. 1,  Hilal  H. S.1, Helal M. H.2, Park D.H. 3, Campet G. 4, Ateeq M. 1, and Zu’bi A. 1

1SSERL, Department of Chemistry, An-Najah N. University, Palestine

2College of Pharmacy and Nutrition, University of Saskatchewan, Canada.

3Dansuk Industrial Co, LTD. #1239-5, Jeongwang-Dong, Shiheung-Si, South Korea.

4Institut de Chimie de la Matie‘re Condense’ıe de Bordeaux (ICMCB), France.

Different methods and strategies were followed for water and soil purification, the best one is the one with higher efficiency and low cost. Photodegradation is one of the most attractive methods.  It involves excitation of the suitable semiconductor by light, before degradation of water or soil organic contaminants occurs. TiO2 nano- and micro-particles have been used for photo-degradation of widely spread water organic contaminants. Due to its wide band gap (~3.2 eV) TiO2 photo-catalytic activity is limited to shorter wavelengths only (UV region). As only ~4% of the solar spectrum falls in the UV region, smaller band gap semiconductors (e.g. CdS, with 2.3 eV) are used to sensitize TiO2 particles. The TiO2/CdS system has been used as catalyst in water purification by photo-degradation of organic contaminants such as methyl orange and Phenazopyridine (Medically active compound). However, the TiO2/CdS system is unstable under photodegradation conditions yielding hazardous Cd2+ ions. Alternative ZnO nanoparticles naked and substrate to different materials like (clay, sand, and activated carbon) were used in photodegradation process; also natural dyes (anthocyanin & Curcumine) were used as sensitizer for the TiO2 nanoparticles. The different prepared nano-catalyst systems were used to photo-degrade various contaminants of water and soil, such as methyl orange, phenazopyridine, paracetamol, phenols, and halo-phenols, with solar radiation. Furthermore, the ZnO nanoparticles were used in water purification and disinfection (from bacteria) by complete mineralization under solar light. Different reaction parameters (such as catalytic efficiency, effects of catalyst concentration, catalyst recovery, contaminant concentration, temperature, pH and complete mineralization) will be discussed together.

Keywords: Photodegradation, Nanoparticles, TiO2, Sensitization, water purification

References:

1) Ahed Zyoud; Nidal Zaatar; Iyad Saadeddin; Cheknane Ali; DaeHoon Park; Guy Campet; HikmatS Hilal, Ph.D ,  CdS-sensitized TiO2 in phenazopyridine photo-degradation: Catalyst efficiency, stability and feasibility assessment. Journal Hazardous Materials, 173, ( 2010), 318-325.

2) Hikmat S. Hilal, Ghazi Y. M. Al-Nour and Ahed Zyoud, Muath H. Helal Iyad Saadeddin, Pristine and supported ZnO based catalysts for phenazopyridine degradation with direct solar light, Conditionally accepted at Solid State Sciences, 12, (2010), 578-586

3) Ahed Zyoud, Nidal Zaatar, Iyad Saadeddin, Muath H. Helal, Guy Campet, Moulki Hakim, DaeHoon Park, Hikmat S. Hilal, Alternative natural dyes in water purification: Anthocyanin as TiO2-sensitizer in methyl orange photo-degradation, Solid State Sciences, 13, (2011), 1268-1275

4) Ahed H Zyoud, Amani Zu’bi, Muath H. S. Helal, DaeHoon Park, Guy Campet,  Hikmat S. Hilal,  Optimizing photo-mineralization of aqueous methyl orange by nano-ZnO catalyst under simulated natural conditions, Journal of Environmental Health Science & Engineering 13, (2015), 46

5) Ahed H. ZYOUD & Hikmat S. HILAL, Investigation of curcumin as sensitizer for anatase TiO2 nanoparticles in photodegradation of of phenazopyridine with visible light, PhytoChem & BioSub Journal Vol. 8(3) 2014, 127-137.

6) Ahed Zyoud, Maysa Ateeq, Muath H. Helal, Hikmat S. Hilal, Photo-catalytic mineralization of phenazopyridine contaminant in soil with direct solar light, Journal of environmental health science and engineering (submitted 2015).

### 7) Ahed Zyoud, Amani Zu’bi, Muath H. S. Helal, DaeHoon Park, Guy Campet and Hikmat S. Hilal, Optimizing photo-mineralization of aqueous methyl orange by nano-ZnO catalyst under simulated natural conditions, Journal of environmental health science and engineering (2015).